## Slide 1
SCIENCE · RECAP
Wood, steel, uPVC and aluminium
How window frames insulate, and how they age
Notes: Four materials behave very differently inside a window frame, and the reason is materials science, because every substance conducts heat at a different rate and reacts differently to moisture and oxygen. Today we look at how a window's insulation is measured, how wood and uPVC behave, what happens to the two metals, and why the frame material alone does not decide how well a window insulates.

## Slide 2
BEFORE WE LOOK AT THE MATERIALS
What decides how well a
window insulates?
Notes: The number that matters is thermal transmittance U, the flow of heat that passes, per square meter of surface, through a structure separating two environments at different temperatures. It is measured in W/m²K, and the lower the number the better the structure insulates. For a whole window this overall transmittance is called Uw, and it is a weighted average between the transmittance of the frame, Uf, and that of the glazing, Ug, plus a small contribution from the interaction between frame, glazing and spacer along the edge of the glass pane. Behind all of it sits the thermal conductivity of each material, meaning the speed at which it transports heat whenever there is a temperature difference between its two faces.

## Slide 3
WHAT WE WILL COVER
01
The number that matters
02
Wood and uPVC
03
Iron and aluminium
04
Not just the frame

## Slide 4
THREE LABELS IN W/M²K, LOWER MEANS BETTER
Uf
The frame alone
Changes with material and thickness
Ug
The glazing alone
Around 2.8 W/m²K in 4-12-4 double glazing
Uw
The whole window
Weighted average of the two, plus the edge
Notes: Uf is the transmittance of the frame alone, Ug of the glazing alone, Uw of the whole window, which is a weighted average of the two plus a contribution from the interaction between frame, glazing and spacer along the edge of the glass. In all three cases the unit is the same, W/m²K, and the lower the value the better the structure insulates. These values are calculated following the EN ISO 10077-1 standard, the simplified method, and EN ISO 10077-2, the finite-element calculation for more complex cases.

## Slide 5
IRON, BEFORE AND AFTER GALVANIZING
Unprotected iron
WITH AIR AND MOISTURE
It oxidizes, it corrodes
NATURAL DEFENCES
No natural resistance
Hot-dip galvanized
WHAT OXIDIZES
The zinc, not the iron
MODERATE CORROSIVITY
Around 60 years, calculated
The zinc is used up in place of the iron, and the setting sets the pace.
Notes: Iron and steel conduct heat far more than wood and uPVC, between 50 and 73 W/m·K, and they have no natural resistance to corrosion. Their oxidation on contact with air and moisture is countered with hot-dip galvanizing, governed by the EN ISO 1461 standard. The mechanism is a sacrificial, or cathodic, protection, because the zinc oxidizes in place of the underlying iron, oxidizing much more slowly than bare iron does. The EN ISO 14713-1 standard assigns each environmental corrosivity class a thickness loss in micrometers per year; for a steel item thicker than 6 mm, in a moderately corrosive environment, class C3, typical of urban or non-aggressive industrial settings, a zinc thickness of 40 to 121 micrometers and an average annual loss of 1.4 micrometers give a calculated durability of around 60 years. Real-world durability varies a lot with the environment, because a coastal, saline or aggressive industrial setting consumes the zinc much faster.

## Slide 6
FALSE MYTH
It isn't the metal that decides.
Aluminium's base thermal conductivity is very high, 209 W/m·K, but the thermal break interrupts the continuity of the profile and brings Uf from around 7.0 down to 2.2-3.9 W/m²K.
Notes: Many people take it for granted that aluminium is always a poor insulator because it is a metal. Its base thermal conductivity, 209 W/m·K, really is very high, the highest among the materials considered here and almost three times that of iron, and an unprotected aluminium frame has a transmittance between 5.2 and 7.0 W/m²K depending on the technical source. The thermal break, though, is a plastic interruption that breaks the continuity of the metal profile and drastically reduces the thermal bridge, bringing transmittance into a range between 2.2 and 3.9 W/m²K. Technical sources do not fully agree on the exact limits, 2.2 to 3.8 according to ENEA, 2.4 to 3.9 according to ACCA. It is not the metal itself that decides, but whether the thermal bridge has been interrupted or not.

## Slide 7
NO THERMAL BREAK
Metal
7.0 W/m²K
Uf around, iron or aluminium
WITH A THERMAL BREAK
Aluminium
2.2-3.9 W/m²K
Uf comparable to wood and uPVC
NO METAL AT ALL
Wood and uPVC
1.2-2.8 W/m²K
Indicative Uf, depends on profile
Notes: Here comes the most counterintuitive figure of all. Despite aluminium conducting heat almost three times more than iron, a whole iron frame and an aluminium frame without a thermal break end up at practically the same Uf, around 7.0 W/m²K, the highest value among the materials considered here. What really decides a metal frame's heat loss is not so much the metal's base conductivity as whether it has a thermal break. Values vary from source to source because they depend on profile thickness, wood species and the number of uPVC chambers, and they should be read as indicative orders of magnitude, not as single absolute figures.

## Slide 8
ALUMINIUM CAN BE REMELTED WITHOUT DEGRADING
95%
less energy, about: compared with producing it from virgin raw material
157,000
MJ per tonne: for primary aluminium, European Aluminium data cited by CIAL
8,540
MJ per tonne: for one tonne of recycled aluminium
Notes: Aluminium can be melted down and reworked without losing its mechanical properties, so in principle it can be recycled indefinitely. According to European Aluminium data cited by the Italian consortium CIAL, producing one tonne of primary aluminium takes around 157,000 MJ of energy, against the 8,540 MJ needed for one tonne of recycled aluminium, an energy saving of about 95%. In 2020, recycling 47,400 tonnes of aluminium packaging, with an 87% melting efficiency, avoided the emission of 355,000 tonnes of CO₂ equivalent. Those last figures are specific to packaging, not window profiles, but the underlying chemical principle, that aluminium can be remelted without degrading, holds for any object made of this metal.

## Slide 9
THE FRAME MATERIAL DOES NOT DECIDE ON ITS OWN
5.8
W/m²K, single-pane glass: the Ug of one pane on its own
2.8
W/m²K, double glazing: around, in a 4-12-4 double-glazed unit
1.7
W/m²K, composite profile: Uf around, aluminium and wood in one frame
Notes: The same technical sources that report these values flag an important limit, because the frame material alone does not determine how well a finished window insulates. The thermal-break technology, how wide it is and what plastic it is made of, and the type of glazing, single pane or double glazing, with or without inert gases such as argon or krypton in the cavity, matter a great deal too. A 4-12-4 double-glazed unit has a Ug of around 2.8 W/m²K against 5.8 W/m²K for single-pane glass, a difference that can matter as much as, or more than, the chosen frame material. Composite or mixed profiles also exist, combining two materials in the same frame, typically aluminium and wood, to bring together the metal's resistance to the elements with the wood's insulating capacity, with a frame-only Uf of around 1.7 W/m²K; a complete window with this kind of frame and double glazing reaches an overall Uw of around 2.5 W/m²K.

## Slide 10
AND NOW, THE REVIEW
Clear in 30 seconds.
Yours in 10 minutes.
A 5-question quiz and 8 flashcards: recaplica.com/en/science/window-frame-materials-comparison/
Sources: ENEA · ACCA/BibLus-net · CIAL · PVC Forum Italia · Infobuild
Notes: To review, the Recap online has the 5-question quiz and the 8 flashcards, with all the full sources at the bottom of the page.